COOL ROOF RATING COUNCIL
PRODUCT LIST

360-673-8660

www.steelscape.com

©2015 Steelscape, LLC All rights reserved. SPS110 April 2015

 

Steelscape is the market leader in high-quality
metallic-coated and pre-painted steel.

Cool Roof Rating Council Product List
Steelscape has four products listed with the Cool Roof Rating Council (CRRC). The values for each product has been tested and verified per CRRC protocol and are listed on the CRRC product directory, www.coolroofs.org/products.

Steelscape Product List:
Product Name	CRRC ID	Initial SR	3 Year SR	Initial Emissivity	3 Year Emissivity	Initial SRI	3 Year SRI	
ZINCALUME®	1014-0001	0.78	0.52	0.06	0.15	75	26	
ZINCALUME® Plus	1014-0002	0.68	0.62	0.30	0.14	65	46	
Vintage®	1014-0003	0.30	0.28	0.70	0.71	22	20	
Sedona Rust Print	1014-0004	0.30	0.28	0.87	0.88	31	28	

The CRRC is responsible for developing accurate and credible methods for evaluating and labeling the solar reflectance and radiative properties of roofing products. At the core of the CRRC is its Product Rating Program, in which manufacturers can label various
roof surface products with radiative property values rated under a strict program administered by the Council. Code bodies, architects, building owners and specifiers can rely on the rating information provided in the CRRC Rated Products Directory.
Should you have any questions regarding this performance data or the CRRC listing, please contact your Steelscape Account Manager.