AN AGED METALLIC LOOK...WITHOUT THE WAIT	

Vintage®

Vintage is an innovative prepainted metal product which
provides warmth and character. A proprietary coating ‘pre- ages’ Steelscape’s TruZinc® metallic coated steel surface
producing a beautiful and durable finish that is also graffiti resistant.
The combination of pigmentation and gloss is what gives our Vintage coated metal a dynamic and aged appearance and has become a top choice for architects and designers.
Vintage coated metal is ideal for roofing and siding applications, as well as unique interior applications.

Achieve your design vision with the durability and affordability of steel.

Vintage is produced in G90 metallic coating weight and comes with a limited warranty.

Vintage®
SRI 22 • 14102

Representation of color may vary due to printing limitations. Actual metal samples are available upon request.

®

VINTAGE®

	steelscape.com	

888-553-5521

©2024 Steelscape, LLC All rights reserved. SPS100 0424 web

steelscape.com

®

VINTAGE®

Substrate:
(ASTM A653)	G90 TruZinc® (HDG) Coated Steel	
Finish:	Proprietary “aged” look using
fluorocarbon prepaint technology	
Surface Appearance:	Smooth and free of blistering and other surface imperfections	
Film Thickness:
(ASTM D5796)	Top System Finish: 0.55 - 0.65 mil

Bottom System Finish: Primer = 0.15 - 0.25 mil
Backer = 0.30 - 0.40 mil	
Specular Gloss:
(ASTM D523)	60 Degree Specular Gloss =
20% - 40%	
Hardness:
(ASTM D3363)	2H - 4H	

Cure Test:
(ASTM D5402)	
100 Double MEK Rubs Minimum	

Abrasion, Falling
Sand:
(ASTM D968)	
65 - 85 liters/mil	
Cross Hatch Adhesion:
(ASTM D3359)	No Tape Off	

Reverse Impact:
(ASTM D2794)	
No Tape Off, 80 inch-pounds of force	
T-Bend Flexibility:
(ASTM D4145)	2T No Tape Off	

Humidity Resistance:
(ASTM D2247)	
1,000 Hours - Passes
(100% RH @ 100 degrees F)	
Salt Spray Resistance:
(ASTM B117)	1,000 Hours - Passes
(5% Salt Spray @ 95 degrees F)	

PERFORMANCE QUALITIES