Matte Barnwood
XWOOBG20

Matte Red Cedar
XWOORC21

Matte Woodgrain
An uncompromising, authentic wood siding alternative.
Matte Woodgrain expands the appeal of metal siding through its detailed pattern, low-gloss finish, and authentic color. Unlike wood, metal is fire-resistant, rot-resistant, termite-resistant, and will never need to be retreated or re-stained.

Steelscape’s Matte Woodgrain series offers an authentic, high-performance finish for metal siding.

www.steelscape.com/woodgrain	®

888-553-5521

steelscape.com

®

Matte Woodgrain Product Details

Product Overview	Two low-gloss metal siding colors featuring a detailed woodgrain pattern design	
Advantages to End Users	An authentic metal siding finish alternative to traditional wood siding. Metal siding offers a maintenance-free, high-performance solution ideal for extreme environments	
Applications	Ideal for metal siding, including board and batten siding, architectural wall accents, metal log cabins, barndominiums, and more	
Paint System	Low-gloss Silicon Modified Polyester (SMP)	
Warranty	25-year film integrity and chalking warranty	
Available Thickness	0.0140” - 0.0296” (29 – 22 Gauge)	
Available Substrates	TruZinc® (G60 or G90) or ZINCALUME® (AZ50)	
Installation	Batch and direction sensitive	
Strippable Film	Standard films suitable	
Production Location	Kalama, Washington	
Matte Woodgrain Product Performance

	Matte Barnwood	Matte Red Cedar	
	XWOOBG20	XWOORC21	
Solar Reflectivity (SR)	0.35	0.27	
Emissivity	0.88	0.87	
Solar Reflectance Index (SRI)	38	26	
Gloss	3	3	
Light Reflectance Value (LRV)	16	11	

Request samples today at steelscape.com