®

COOL ROOF RATING COUNCIL PRODUCT LIST

888-553-5521

steelscape.com

©2024 Steelscape, LLC All rights reserved. SPS110 0124 web

Steelscape has four products listed with the Cool Roof Rating Council (CRRC). The values for each product has been tested and verified per CRRC protocol and are listed on the CRRC product directory, www.coolroofs.org/products.

Product Name	CRRC ID	Initial SR	3 Year SR	Initial Emissivity	3 Year Emissivity	Initial SRI	3 Year SRI	

Steelscape Product List:
								
ZINCALUME®	1014-0001	0.78	0.52	0.06	0.15	75	26	
ZINCALUME® Plus	1014-0002	0.68	0.62	0.30	0.14	65	46	
Vintage®	1014-0003	0.30	0.28	0.70	0.71	22	20	
Sedona Rust Print	1014-0004	0.30	0.28	0.87	0.88	31	28	
Natural Matte® Color Collection							
Shale	1014-0005	.35	.35	.83	.83	35	35	
Basalt	1014-0006	.25	.25	.83	.83	22	22	
Graphite	1014-0007	.25	.25	.83	.83	22	22	
Carbon	1014-0008	.25	.25	.83	.83	22	22	
Frost	1014-0009	.70	.63	.83	.83	84	75	
Ore	1014-0010	.25	.25	.83	.83	22	22	

The CRRC is responsible for developing accurate and credible methods for evaluating and labeling the solar reflectance and radiative properties of roofing products. At the core of the CRRC is its Product Rating Program, in which manufacturers can label various roof surface products
with radiative property values rated under a strict program administered by the Council. Code bodies, architects, building owners and specifiers can rely on the rating information provided in the CRRC Rated Products Directory.
If you have questions, please contact your Steelscape Account Manager.