®

An Introduction to the Steelscape FEVE Coatings Family

888-553-5521

steelscape.com

©2024 Steelscape, LLC ZINCALUME® is a registered trademark of BlueScope Steel Ltd. All rights reserved. SPS111 0624

	What is FEVE?	

coatings. Specifically developed for exterior applications, these coatings feature the same high-performance carbon- fluorine bond found in premium PVDF paints. This provides excellent durability against the effects of corrosion, UV

FLUOROETHYLENE VINYL ETHER (shortened to FEVE) refers to a product family of tinted translucent

light, and humidity. Unlike traditional paint systems, FEVE coatings are developed to provide color and performance
without the use of a primer. This enables the distinctive visual appeal of the base metal to be apparent while providing enhanced color depth and a unique interaction with light.

Steelscape offers three distinct products featuring this exceptional architectural finish.

VINTAGE®	MORE INFORMATION ➜ Vintage Product Page

FINISH DESCRIPTION: Vintage® recreates the warmth and character of aged metal. Extensively used in metal building design for its versatile color and as a cost-effective substitute for zinc. Vintage offers greater color vibrancy and depth compared to traditional gray and bronze paint colors.

VINTAGE®

TECHNICAL DETAILS: A semitransparent coating over Steelscape’s TruZinc® galvanized steel. Offered in 24-gauge thickness (0.0236") with a G90 coating weight (the industry standard for galvanized corrosion protection). Vintage carries a limited 20-year finish warranty and is produced at Steelscape’s Kalama, WA facility.

LEGACY

EVOLUTION

 VINTAGE® HERITAGE	MORE INFORMATION ➜ Vintage Heritage Product Page	

FINISH DESCRIPTION: Vintage® Heritage is the next generation of Vintage. Featuring a printed design beneath the popular Vintage finish, it offers a more pronounced design for greater finish definition.
Available in Two Patterns:
Legacy: A varied mottled pattern creating a spangled effect.
Evolution: Brushed varied parallel lines creating a striated effect.
TECHNICAL DETAILS: A printed design beneath a semitransparent coating. Produced on TruZinc® metallic coated steel in either 22 or 24-gauge thickness (0.0296" or 0.0236"). Both designs feature the same limited 20-year finish warranty as Vintage.

SUMMARY	VINTAGE®	VINTAGE HERITAGE®	
SUBSTRATE	TruZinc	TruZinc	
COATING WEIGHT	G90	G90	
THICKNESS	0.0236” (24ga)	0.0236” (24ga)
0.0296” (22ga)	
PRODUCTION	Kalama, WA	Kalama, WA	
FINISH WARRANTY	20-year coating	20-year coating	
CORROSION WARRANTY	N/A	N/A